FLOOR PREMIUM EPOXY DATA SHEET

PRODUCT DESCRIPTION

FLOOR PREMIUM EPOXY is formulated with 100% solids thermo-setting epoxy resin and hardener containing no oils, or other non-recovering modifiers. FLOOR PREMIUM EPOXY upgrades the surface of existing floors adding little height and weight and provides superior protection. These products are manufactured as a monolithic, decorative and chemical-resistant floor coating. FLOOR PREMIUM EPOXY has additives that support minimal substrate expansion and contraction without effecting the bond and integrity of the coating.

SURFACE PREPARATION

All surfaces must be clean, dry and structurally sound. Curing compounds, grease, oil, dirt, vegetation, asphalt, paint, or other foreign matter must be removed in order to assure good adhesion. Use CLEANER X to thoroughly clean surface, ETCH X to deep clean and open the pores of the concrete. New concrete must be finished with a neat, clean, sand finish and allowed to cure 21 to 28 days.

MIXING PROCEDURES

Upon opening, stir thoroughly, as products may settle. Always use a separate mixing tool for parts A & B.

Primer: For porous surfaces, blend two parts BONDING PRIMER Base A with one part BONDING PRIMER Hardener and apply following BONDING PRIMER application instructions.

After stirring FLOOR PREMIUM EPOXY Hardener B thoroughly, mix one part FLOOR PREMIUM EPOXY Hardener B with two parts FLOOR PREMIUM EPOXY Base A. Mix thoroughly using a paddle mixer or drum mixing machine for 3-5 minutes. Use a slow speed mixer to eliminate whipping air into Epoxy.

APPLICATION PROCEDURES

Place the mixed material on the surface a small amount at a time, only mix an amount that can be applied in 20 minutes. Apply using a 3/8 inch nap roller, brush, or epoxy sprayer. Any excess material should be completely rolled out. FLOOR PREMIUM EPOXY will cure under normal conditions to allow walking traffic in approximately 12 hours. Maximum physical and chemical properties will be obtained after 14 days curing time. Always apply in good ventilation and never near an open flame. Not recommended for exterior use with direct sunlight exposure.

Physical Specifications

Compressive Strength - 18,000 p.s.i.

Flexural Strength - 5,300 p.s.i.

Adhesion to Concrete - 100% Bond

Adhesion to Wood - 100% Bond

Abrasion Resistance - Using a H-22 grit stone wheel under a 1,000 gram load where factor

loss per 1 000 cycles equal 1,520 milligrams

Impact Resistance - Using a 2-1/2 bond, steel ball falling from a height of 24 inches - no effect

Chemical Resistence:

Acetone		No Effect		Skydrol			No Effect

Alcohols		No Effect		Milk, Sour or Fresh	No Effect

Aliphatic Solvents	No Effect		Soap and Detergents	No Effect

Alum			No Effect		Sugar			No Effect

Ammonia		No Effect		Urine			No Effect

Aromatic Solvents	No Effect		Salt Water		No Effect

Boric Acid		No Effect		10% Nitric Acid		Discolored

Cooking Fats and Oil	No Effect		Crude Oil		No Effect

Blood	No Effect	Trisodium 		Phosphate 5%		No Effect

Formaldehyde 37%	No Effect		10% Sodium Hydroxide	No Effect

Hydrocarbon Fuels	No Effect		Caustic (NaOH)	50% 	No Effect

*For a Non-Skid Traction Safety Finish, add non-slip granules Non slip aggregates can be purchased from AmeriCoatings and mixed into the epoxy or can be broadcast into the wet epoxy.