EXPANSION JOINT COMPOUND

PRODUCT DESCRIPTION

EXPANSION JOINT COMPOUND is a two-component, tintable, primerless, flexible, self-leveling, adhesive compound. EXPANSION JOINT COMPOUND is made from 100% solid resins and is resistant to most chemicals in severe environments. EXPANSION JOINT COMPOUND is a polysulfide enhanced formulation that forms a bond that will accommodate a wide variety of expansions without loss of integrity through contraction, sheer, vibration, or compression.  EXPANSION JOINT COMPOUND bonds to metal, wood, concrete, plastics, masonry and other elastomerics. EXPANSION JOINT COMPOUND is specially formulated for exterior as well as interior applications. EXPANSION JOINT COMPOUND can be purchased in conveniently packaged dual Caulk Grade cartridges.

SURFACE PREPARATION

All surfaces must be clean, dry and structurally sound to apply EXPANSION JOINT COMPOUND. Curing compounds, grease, oil, dirt, vegetation, asphalt, paint, or other foreign matter must be removed in order to assure good adhesion.

MIXING PROCEDURES

Upon opening, mix thoroughly, as products may settle. Always use a separate mixing tool for parts A & B.

Blend one part EXPANSION JOINT COMPOUND Base A Resin to one part EXPANSION JOINT COMPOUND B Hardener.  Mixing shall be by slow speed drill and paddle under continuous agitation for 30 - 60 seconds. Complete mixing approximately five minutes prior to application.

APPLICATION PROCEDURES

After joint to be filled is clean and dry from all debris:

1. Install closed cell Polyethylene joint backer rod in the joint using a size that is approximately 30% larger than the joint width. The backing should be recessed below the lip of the joint a distance of ½ the width of the joint.

2. Apply 2" wide masking tape to the edges of the joint.

3. If applying by using a caulk gun, insert plunger into mixture, drawing out mixed material in caulk cartridge.

4. Tool the joint with a blade or strike off tool, the width of the joint, to force the sealant down into the joint and work out any air pockets. The tool should be kept wet with IPA or xylene to prevent sticking.

5. After tooling the sealant should be flush with the level of the joint sides and be smooth and free from pinholes or voids with complete continuous contact.

6. Remove the masking tape before the sealant starts to set - (approximately 40 minutes at 77°F).

7. Clean any residue on the surrounding area with xylene.

8. Clean tools periodically during the application before the material starts to set with xylene.

9. EXPANSION JOINT COMPOUND is available in caulk and pourable grade. If applying using a Caulk Gun and supplied cartridge, follow the product instructions on the cartridge.

PRECAUTIONS
EXPANSION JOINT COMPOUND is not compatible with asphalt and cannot be used in asphalt concrete pavement or with asphalt-impregnated expansion joint fillers.